Supplementary Information

Experimental study on thermal and mechanical properties of tailings-based cemented paste backfill with CaCl2·6H2O/expanded vermiculite shape stabilized phase change materials

Xiaoyan Zhang1), Tianrun Cao1), Lang Liu1,2),(, Baoyun Bu1), Yaping Ke1), and Qiangqiang Du3)

1) Energy School, Xi’an University of Science and Technology, Xi’an 710054, China

2) Key Laboratory of Western Mines and Hazards Prevention, Ministry of Education of China, Xi’an 710054, China

3) School of Architecture and Civil Engineering, Xi’an University of Science and Technology, Xi’an 710054, China

( Corresponding author: Lang Liu      E-mail: liulang@xust.edu.cn

Fig. S1 Particle size distribution curve of tailings.

Fig. S2. Particle size distribution curve of expanded vermiculite.

Fig. S3. The preparation process of CEV.

Fig. S4. Schematic diagram of effective specific heat capacity of materials.

Fig. S5. Specific heat capacity of CPB with temperature under different CEV addition ratios with (a) cement-tailing ratio of 1:6 and (b) cement-tailings ratio of 1:8

Table S1. Chemical composition of tailings

| Composition | SiO2 | Al2O3 | CaO | Fe2O3 | MgO | SO3 | TiO2 | K2O | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Content / % | 56.32 | 16.54 | 8.76 | 5.56 | 4.14 | 3.02 | 1.16 | 1.08 | 3.42 |

Table S2. Chemical composition of cement

| Composition | CaO | SiO2 | Al2O3 | Fe2O3 | MgO | Others |
| --- | --- | --- | --- | --- | --- | --- |
| Content / % | 65.12 | 22.36 | 5.53 | 3.46 | 1.27 | 2.26 |