Supplementary Information

Realizing high-performance Na3V2(PO4)2O2F cathode for sodium-ion batteries via Nb-doping

Jie Wang1,2),*, Yifeng Yuan1),*, Xianhui Rao1), Min’an Yang1), Doudou Wang1), Ailing Zhang1), Yan Chen1), Zhaolin Li1,2), and Hailei Zhao1,2),

1) School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing 100083, China

2) Beijing Municipal Key Lab of Advanced Energy Materials and Technologies, Beijing 100083, China

*These authors contributed equally to this work.

Corresponding author: Hailei Zhao     E-mail: hlzhao@ustb.edu.cn

Fig. S1.  Rietveld refined patterns of (a) NVPOF/rGO and (b) NVN10POF/rGO samples.

Fig. S2.  FESEM images of the synthesized (a) NVPOF/rGO, (b) NVN05POF/rGO, and (c) NVN10POF/rGO materials.

Fig. S3.  TEM image of the NVPOF/rGO material.

Fig. S4.  TG curves of the synthesized NVN05POF/rGO and NVPOF/rGO materials.

Fig. S5.  Charge/discharge curves of the NVPOF/rGO electrode at different cycles.

Fig. S6.  Charge/discharge curves of the (a) NVN05POF/rGO and (b) NVPOF/rGO electrode at different current rates.

Fig. S7.  Long-term cycling performance of the NVPOF/rGO electrode at 5 C.

Fig. S8.  CV curves of the (a) NVN05POF/rGO and (b) NVPOF/rGO electrodes at a scan rate of 0.1 mV·s−1.

Fig. S9.  Equivalent circuit for EIS data fitting.

Fig. S10.  Coulombic efficiency of the NVN05POF/rGO electrode under the different test conditions: (a) charge at 0.5 C and discharge at 0.5, 1, 2, 5, and 10 C, respectively; (b) discharge at 0.5 C and charge at 0.5, 1, 2, 5, and 10 C, respectively.

Fig. S11.  Long-term cycling performance of the NVN05POF/rGO electrode at 10 C/10 C (charge rate/discharge rate).

Table S1.  Structural parameters of the synthesized Na3V2−xNbx(PO4)2O2F/rGO (x = 0, 0.05, 0.1) samples from XRD Rietveld refinement

| Sample | Lattice constant |  |  | Refinement factors |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | a = b / Å | c / Å | V / Å3 | Rwp / % | Rp / % | 2 |
| Na3V2(PO4)2O2F | 6.3658(6) | 10.6355(5) | 430.99(7) | 9.20 | 7.31 | 2.786 |
| Na3V1.95Nb0.05(PO4)2O2F | 6.3681(8) | 10.6358(7) | 431.32(5) | 9.79 | 7.57 | 3.344 |
| Na3V1.9Nb0.1(PO4)2O2F | 6.3756(8) | 10.6381(8) | 432.43(5) | 9.96 | 7.56 | 3.687 |

Table S2.  Atomic ratio of Nb and V in Na3V2−xNbx(PO4)2O2F/rGO (x = 0.05, 0.1) samples derived from ICP-OES results

| Sample | Nb : V |
| --- | --- |
| Na3V1.95Nb0.05(PO4)2O2F/rGO | 0.05:0.95 |
| Na3V1.9Nb0.1(PO4)2O2F/rGO | 0.088:0.912 |