Supporting Information

Boosting thermoelectric efficiency of Ag2Se through cold sintering process with Ag nano-precipitate formation

Dejwikom Theprattanakorn1,2), Thanayut Kaewmaraya1,2), and Supree Pinitsoontorn1,2),

1) Department of Physics, Faculty of Science, Khon Kaen University, Khon Kaen 40002, Thailand

2) Institute of Nanomaterials Research and Innovation for Energy (IN-RIE), Khon Kaen University, Khon Kaen 40002, Thailand

Corresponding author: Supree Pinitsoontorn  E-mail: psupree@kku.ac.th

Fig. S1.  X-ray diffraction (XRD) pattern of as-synthesized Ag2Se powder along with a reference pattern.

Table S1.  Rietveld refinement parameters from XRD results of the as-synthesized Ag2Se powder and Ag2Se powders after cold sintering process (CSP)

| Sample | a / Å | b / Å | c / Å | Volume / Å3 | Rp / % | Rwp / % | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| As-synthesized Ag2Se powder | 4.334 | 7.066 | 7.770 | 237.9 | 4.54 | 5.89 | 1.97 |
| Ag:0% | 4.333 | 7.064 | 7.767 | 237.8 | 8.19 | 10.07 | 1.91 |
| Ag:0.5% | 4.328 | 7.065 | 7.777 | 237.8 | 7.82 | 9.66 | 2.26 |
| Ag:1% | 4.327 | 7.066 | 7.780 | 237.8 | 7.04 | 8.80 | 1.93 |
| Ag:2% | 4.327 | 7.068 | 7.784 | 238.1 | 6.71 | 8.43 | 1.76 |

Note: Here, a, b, c represent lattice parameters, Rp, Rwp and 2 represent profile R-factor, weighted profile R-factor and goodness of fit.

Table S2.  Densities and chemical compositions of the CSP Ag2Se pellets.

| Sample | Theoretical density / (gcm3) | Experimental density / (gcm3) | Relative density / % | Ag / at% | Se / at% | Molar ratio Ag:Se |
| --- | --- | --- | --- | --- | --- | --- |
| Ag:0% | 8.22 | 7.62 ± 2.947 | 92.70 | 66.89 | 33.11 | 2.006:1 |
| Ag:0.5% | 8.23 | 7.47 ± 1.584 | 90.76 | 68.60 | 31.40 | 2.057:1 |
| Ag:1% | 8.24 | 7.32 ± 2.973 | 88.83 | 69.86 | 30.10 | 2:096:1 |
| Ag:2% | 8.26 | 7.34 ± 2.840 | 88.86 | 70.79 | 29.21 | 2.124:1 |

Note: Theoretical densities were calculated from the density of Ag2Se (8.22 gcm3) and Ag (10.49 gcm3) [S1], whereas experimental densities were measured using an Archimedes’ method. Chemical compositions were determined by energy-dispersive X-ray spectroscopy (EDS) mapping analyses.

Fig. S2.  A scanning electron microscope (SEM) image of as-synthesized Ag2Se powder.

Fig. S3. A bright-field transmission electron microscope (TEM) image showing the crystallite size of the Ag:0% sample. The (121) plane of the Ag2Se crystal is observed (inset).

Fig. S4.  A cross-sectional SEM image of the Ag:0% sample.

Fig. S5.  Grain size distribution from SEM images of the CSP samples: (a) Ag:0%, (b) Ag:0.5%, (c) Ag:1%, (d) Ag:2%. Here, SD represents standard deviation.

References

[S1] J. Brillo, I. Egry and I. Ho, Density and Thermal Expansion of Liquid Ag–Cu and Ag–Au Alloys, Int. J. Thermophys., 27(2006), No.2, p.494.