Supplementary Information

Effect of Ca/Mg molar ratio on the calcium-based sorbents

Yumeng Li1,2), Qing Zhao1,2,3),(, Xiaohui Mei1,2), Chengjun Liu1,2), Henrik Saxén4), and Ron Zevenhoven4)

1) Key Laboratory for Ecological Metallurgy of Multimetallic Mineral (Ministry of Education), Northeastern University, Shenyang 110819, China

2) School of Metallurgy, Northeastern University, Shenyang 110819, China

3) Institute for Frontier Technologies of Low-Carbon Steelmaking, Northeastern University, Shenyang 110819, China

4) Process and Systems Engineering Laboratory, Åbo Akademi University, Åbo/Turku 20500, Finland

Table S1.  r2 for different reaction orders of the Aveami-Erofeev model applied to the first stage adapted to the experimental results obtained at different temperatures

| r2 | First stage |
| --- | --- |
|  | n=4 | n=3 | n=2 | n=2/3 | n=1/2 | n=1/3 | n=1/4 |
| r2750℃ | 0.8532 | 0.8298 | 0.9593 | 0.9864 | 0.8713 | 0.7802 | 0.7045 |
| R2700℃ | 0.7102 | 0.7608 | 0.8321 | 0.9744 | 0.9869 | 0.9771 | 0.9478 |
| R2650℃ | 0.6835 | 0.7347 | 0.8083 | 0.9645 | 0.9844 | 0.9860 | 0.9649 |

Table S2.  r2 for different reaction orders of the Aveami-Erofeev model applied to the second stage adapted to the experimental results obtained at different temperatures

| r2 | Second stage |
| --- | --- |
|  | n=4 | n=3 | n=2 | n=2/3 | n=1/2 | n=1/3 | n=1/4 |
| r2750℃ | 0.9302 | 0.9360 | 0.9468 | 0.9895 | 0.9981 | 0.9391 | 0.8458 |
| r2700℃ | 0.8223 | 0.8272 | 0.8366 | 0.8856 | 0.9054 | 0.8368 | 0.9103 |
| r2650℃ | 0.8960 | 0.8990 | 0.9047 | 0.9335 | 0.9445 | 0.9048 | 0.9471 |

Table S3.  Values of K and -ln K of Aveami-Erofeev model at different temperatures

| T / K | First stage |  | Second stage |
| --- | --- | --- | --- |
|  | 1/(T×10-3) | K | -ln K |  | 1/(T×10-3) | K | (ln K |
| 1023.15 | 0.9774 | 0.0243 | 3.7173 |  | 0.9679 | 0.0133 | 4.3200 |
| 973.15 | 1.0276 | 0.0194 | 3.9425 |  | 1.0276 | 0.0089 | 4.7217 |
| 923.15 | 1.0832 | 0.0139 | 4.2759 |  | 1.0832 | 0.0056 | 5.1850 |

Fig. S1.  SEM image and EDS element mapping of the calcium-based sorbent prepared from steel slag leachate.