Supplementary Information

Core-shell mesoporous carbon hollow spheres as the Se host for advanced Al-Se batteries

Haiping Lei1,2), Tianwei Wei2), Jiguo Tu1), and Shuqiang Jiao1),

1) State Key Laboratory of Advanced Metallurgy, University of Science and Technology Beijing, Beijing 100083, China

2) School of Metallurgical and Ecological Engineering, University of Science and Technology Beijing, Beijing 100083, China.

(Received: 25 September 2023; Revised: 21 November 2023; Accepted: 13 December 2023)

Fig. S1.  (a) The SEM image of as-prepared SiO2@RF. (b) The corresponding EDS elemental mapping images of the as-prepared SiO2@RF. (c) Typical SEM image of SiO2@RF@TiO2. (d) The corresponding EDS elemental mapping images of SiO2@RF@TiO2.

Fig. S2.  The SEM images (a–c) and corresponding EDS elemental mapping images (d−i) of the as-prepared SiO2@C@TiN.

Fig. S3.  (a) The SEM images and corresponding EDS elemental mapping images of the as-prepared Se@C@TiN. (b) The corresponding representative EDS spectrum of the as-prepared Se@C@TiN.

Table S1.  The Se, C, N, Ti contents of Se@C@TiN by EDS.

| Samples | wt% | at% |
| --- | --- | --- |
| Se | 63.9 | 22.78 |
| C | 30.86 | 72.34 |
| N | 1.27 | 2.55 |
| Ti | 3.97 | 2.33 |

Fig. S4.  XRD patterns of the C@TiN samples.

Fig. S5.  (a) N2 adsorption/desorption isotherms of as-prepared C@TiN. (b) The pore diameter distribution of as-prepared C@TiN.

Fig. S6.  Raman spectrum of as-prepared Se@C@TiN.

Fig. S7.  Survey XPS spectra of Se@C@TiN.

Fig. S8.  (a) CV curves of Al-C@TiN batteries between 0.01~2.4 V vs Al3+/Al at a scan rate of 1 mV s−1. (b) The galvanostatic charge/discharge curves of Al-C@TiN batteries at the current densities of 100, 200, and 300 mA g−1.

Fig. S9.  (a) The galvanostatic charge/discharge curves of Al-Se@C batteries at a current density of 1000 mA g−1. (b) The corresponding cycling performance.

Fig. S10.  The rate performances of (a) Al-Se@C@TiN and (b) Al-Se batteries at current densities of 1000, 1200, and 1400 mA g−1.图左侧也有坐标变量和单位吧，若有，请补上，同时把右侧坐标变量和单位转180度

Table S2.  Comparison of electrochemical performances of Se@C@TiN positive electrode with previous Se-based positive electrodes.

| Positive electrode | Electrolyte | Separator | Voltage range (V) | Discharge capacity (mAh·g−1) | Current density (mA·g−1) | Cycles |
| --- | --- | --- | --- | --- | --- | --- |
| This work (Se@C@TiN) | [EMIm]Cl /AlCl3, 1: 1.3 by mole | glass fiber (GF/A) | 0.01–2.4 | 137 | 1000 | 120 |
| Se@CMK-3[1] | [EMIm]Cl /AlCl3, 1: 1.3 by mole | Whatman GF/D | 0.05–1.5 | 600 | 67.5 | 9 |
| MCF-7/Se[2] | [EMIm]Cl /AlCl3, 1: 1.1 by mole |  | 1.0–2.3 | 152 | 500 | 2000 |
| Se nanowires and mesoporous carbon (Se/CMK-3)[3] | [EMIm]Cl -AlCl3, 1:1.1 by mole | Glass fiber (Filtech) | 1.0–2.3 | 124 | 200 | 50 |
| One-dimensional hollow Se@C nanotube (Se@CT)[4] | [EMIm]Cl /AlCl3, 1: 1.3 by mole | Whatman glass fiber (GF/C) | 0.5–2.3 | 162.9 | 500 | 200 |

Fig. S11.  (a) XRD spectra of positive electrode after fully charged and discharged. (b) XPS spectra of Al 2p of positive electrode after fully charged and discharged. (c) XPS spectra of Cl 2p of positive electrode after fully charged and discharged.

References

[1] S.Q. Liu, X. Zhang, S.M. He, et al., An advanced high energy-efficiency rechargeable aluminum-selenium battery, Nano Energy, 66(2019), art. No. 104159.

[2] Y.Q. Kong, A.K. Nanjundan, Y. Liu, H. Song, X.D. Huang, and C.Z. Yu, Modulating ion diffusivity and electrode conductivity of carbon Nanotube@Mesoporous carbon fibers for high performance aluminum–selenium batteries, Small, 15(2019), No. 51, art. No. 1904310.

[3] X.D. Huang, Y. Liu, C. Liu, J. Zhang, O. Noonan, and C.Z. Yu, Rechargeable aluminum-selenium batteries with high capacity, Chem. Sci., 9(2018), No. 23, p. 5178.

[4] Z.Y. Li, J. Liu, X.G. Huo, J.L. Li, and F.Y. Kang, Novel one-dimensional hollow carbon nanotubes/selenium composite for high-performance Al-Se batteries, ACS Appl. Mater. Interfaces, 11(2019), No. 49, p. 45709.

Corresponding author: Shuqiang Jiao   E-mail: sjiao@ustb.edu.cn