Supplementary Information

Dielectric loss enhancement induced by the microstructure of CoFe2O4 foam to realize broadband electromagnetic wave absorption

Bin Shi1), Hongsheng Liang2), Zijun Xie1), Qing Chang1,2),(, and Hongjing Wu2),(

1) College of Chemistry and Chemical Engineering, Shaanxi Key Laboratory of Chemical Reaction Engineering, Yan’an University, Yan’an 716000, China

2) MOE Key Laboratory of Material Physics and Chemistry Under Extraordinary, School of Physical Science and Technology, Northwestern Polytechnical University, Xi’an 710072, China

( Corresponding authors: Qing Chang   E-mail: changqingyau@126.com;    Hongjing Wu    E-mail: wuhongjing@nwpu.edu.cn

Related Figures

Fig. S1.  Sol, xerogel, and CoFe2O4 foam of S1.5.

Fig. S2.  Real part (a) and imaginary part (b) of complex permittivity; C0 values (c); impedance matching of S1.0 (d) and S1.5 (e); attenuation constant (f).

Related Tables

Table S1.  Peak area of bonded oxygen and oxygen vacancy

| Sample | M–O | Oxygen vacancy | Oxygen vacancy/M–O |
| --- | --- | --- | --- |
| S0.5 | 27197.15 | 6909.50 | 0.25 |
| S1.0 | 9095.33 | 9427.23 | 1.04 |
| S1.5 | 56831.82 | 21529.38 | 0.38 |

Table S2.  Saturation magnetization and coercivity of the as-obtained CoFe2O4 foams and reported bulk CoFe2O4

| Sample | Ms (emu/g) | Hc (Oe) |
| --- | --- | --- |
| S0.5 | 78.29 | 571.40 |
| S1.0 | 56.35 | 792.72 |
| S1.5 | 63.40 | 896.44 |
| Bulk CoFe2O4 | 82 | 304 |

Table S3.  Specific surface area of the as-obtained CoFe2O4 foams

| Sample | Specific surface area (m²/g) |
| --- | --- |
| S0.5 | 6.02 |
| S1.0 | 38.49 |
| S1.5 | 8.21 |

Table S4.  EMW absorption performance of the as-obtained CoFe2O4 foams and CoFe2O4-baesd absorbents in literature.

| Samples | EAB (GHz) | Thickness (mm) | Reference |
| --- | --- | --- | --- |
| CoFe2O4 | 2.6 | 2.5 | 11 |
| CoFe2O4/C | 4.2 | 1.5 | 39 |
| RGO/CoFe2O4/ZnS | 5.5 | 2.0 | 37 |
| CoFe2O4/rGO | 5.8 | 2.8 | 13 |
| rGO/CoFe2O4 | 6.16 | 2.0 | 38 |
| MoS2/CoFe2O4 | 6.26 | 1.6 | 15 |
| CoFe2O4/graphene | 5.4 | 1.7 | 19 |
| CoFe2O4/rGO | 6.8 | 2.2 | 16 |
| CoFe2O4/N-rGO aerogels | 6.48 | 2.2 | 36 |
| CoFe2O4@1T/2H-MoS2 | 4.56 | 1.6 | 14 |
| CoFe2O4@rGO | 6.3 | 2.1 | 31 |
| 4CoFe2O4/6Co4Fe6 | 4.16 | 1.45 | 28 |
| CoFe2O4/C | 3.6 | 2.5 | 32 |
| S0.5 | 7.3 | 2.1 | This work |
| S1.5 | 5.0 | 1.7 |  |

Related formula

S(1)

where f, μ0, σ, and d represent the frequency, permeability in vacuum, electric conductivity, and diameter of the nanoparticle, respectively.

The attenuation constant was calculated according to the equation below:

S(2)

where f is the frequency, c is the velocity of the light, ε′ and ε″ are the complex permittivity and µ′ and µ″ are the complex permeability.