Supplementary Information

Quickly obtaining densely dispersed coherent particles in steel matrix and its related mechanical property

Xiaoxiao Wang and Qingsong Huang

School of Chemical Engineering, Sichuan University, Chengdu 610065, China

Fig. S1.  STEM images of second phase nanoparticle: (a1) STEM image of the as-cast Fe–TYMO steel; (a2) STEM image of a particle with size of about 2.72 nm in the yellow dashed line box in (a1); (a3) atomic-resolution STEM image of the particle pointed by the yellow arrow in (a2), with the [111] zone axis; (a4, a5) cross correlation images from yellow square (particle position) and blue square in (a3), respectively; (b1) STEM image of the as-cast Fe–TYMO steel; (b2) STEM image of a particle with size of about 5.05 nm pointed by the yellow arrow in (b1); (b3) atomic-resolution STEM image of the particle pointed by the yellow arrow in (b2), with the [111] zone axis; (b4, b5) cross correlation images from yellow square (particle position) and blue square in (b3), respectively.

Fig. S2.  STEM images of second phase nanoparticle in rolled (700℃,10 s-1) Fe-TYMO steel: (a1) STEM image of a particle with size of about 7.62 nm; (a2) atomic-resolution STEM image of the particle pointed by the yellow arrow in (a1), with the [001] zone axis; (a3, a4) cross correlation images from yellow square (particle position) and blue square in (a2), respectively; (b1) STEM image of a particle with size of about 3.91 nm; (b2) atomic-resolution STEM image of the particle pointed by the yellow arrow in (b1), with the [001] zone axis; (b3, b4) cross correlation images from yellow square (particle position) and blue square in (b2), respectively.

Fig. S3.  HAADF and EDS mapping images of as-cast Fe–TYMO steel sample. The mass fraction of Fe, Y, Ti, Mn, and O element corresponds to the selected region area #1.

Fig. S4.  HAADF and EDS mapping images of rolled (700℃, 10 s-1) Fe–TYMO steel sample at strain rate of 10 s-1 at 700 ℃. The mass fraction of Fe, Y, Ti, Mn, and O element corresponds to the selected region area #1.

Fig. S5.  Warm-Rolling stress-strain curves of Fe–TYMO steel at strain rate of 0.1, 1, and 10 s-1 at 700℃.

Fig. S6.  Electron back-scattering diffraction (EBSD) IPF (inverse pole figure) maps and GB (grains boundary) maps and misorientation angle histogram of rolled Fe–TYMO steel and rolled pure ferrite steel grains: (a) Fe–TYMO steel (700℃, 0.1 s-1); (b) Fe–TYMO steel (700℃, 1 s-1); (c) Fe–TYMO steel (700℃, 10 s-1); (d) pure ferrite steel (700℃, 10 s-1). All the scale bars in the maps represent 300 μm.

Fig. S7.  (a) Compressive engineering stress–strain curve of the rolled pure ferrite steel at strain rate of 0.1, 1, and 10 s-1 under 700℃ respectively; (b) the first derivative of the compressive engineering stress–strain curve of the rolled pure ferrite steel; (c) the second derivative of the compressive engineering stress–strain curve of the rolled pure ferrite steel (the inset shows enlargement of the selected area in the purple dashed box).

Table S1.  Compressive yield strength (σ0.2) and compressive strength (σm) of as-cast, as-rolled, and as-annealed (annealed at 700℃ for 20 min) Fe–TYMO steels

| Compression test | As-cast | As-rolled |  |  | As-annealed |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 0.1 s-1 | 1 s-1 | 10 s-1 | 0.1 s-1 | 1 s-1 | 10 s-1 |
| σ0.2 (MPa) | 303 | 397 | 514 | 569 | 425 | 415 | 385 |
| σm (MPa) | 1037 | 1202 | 1220 | 1258 | 1216 | 1174 | 1112 |

Corresponding author: Qingsong Huang    E-mail: qshuang@scu.edu.cn