Supplementary Information

Modified Al negative electrode for stable high-capacity Al–Te batteries

Xuefeng Zhang and Shuqiang Jiao,

State Key Laboratory of Advanced Metallurgy, University of Science and Technology Beijing, Beijing 100083, China.

Corresponding Author: Shuqiang Jiao   E-mail: sjiao@ustb.edu.cn

Fig. S1.  Schematic diagram of the precipitation process of elemental Te on the negative electrode.

Fig. S2. Local amplification of voltage profiles of Al|Al symmetric cells using different electrolytes: (a) Al–Al-FE; (b) Al–Al-DE.

Fig. S3. SEM images of Al–Al symmetrical cells using different electrolytes: (a) fresh electrolyte; (b) dissolved electrolyte with Te.

Fig. S4. (a) SEM image of TiB2 powder. (b) Partial enlargement of (a).

Fig. S5. SEM image with EDS mappings of TB layer.

Fig. S6. SEM image of the surface of Al foil from Al-TB electrode after cycling in Al–TB‖Al–TB cells.

Fig. S7. CVs of Al–Te battery using bare Al negative electrode.

Fig. S8. Corresponding charge/discharge curves of Al–Te battery employed bare Al as the negative electrode at current density of 0.5–2.0 A·g−1.

Fig. S9. SEM images of AB-PVDF-modified separator: (a) side view; (b) top view.

Fig. S10. Electrochemical performance of blank batteries: (a) rate performance; (b) corresponding charge/discharge curves.

Fig. S11. Rate performance of the optimized Al–Te batteries by modified negative and separator: (a) rate performance at current density of 0.5–2.0 A·g−1; (b) corresponding charge/discharge curves.

Fig. S12. SEM image (a) and corresponding DES mapping (b–d) of bare Al negative electrode after cycling.

Fig. S13. SEM image with EDS mapping of metal Al surface after cycling in Al/TB–Te battery.

The weaker and more evenly distributed Te signal in Al/TB electrode compared with bare Al (Fig. S11) demonstrated an effective protection of TB layer to metal Al.

Fig. S14. EDS mapping of TiB2 particle after cycling in TB layer.

Fig. S15. TOF-SIMS mappings of TB.

There are four chemical signals were observed in SIMS mapping, such as –OH, C=N, BO2, and Al–Cl, which indicated that the SEI on the surface of TB layer are mainly related with these chemical signals.

Table S1. State-of-the-art of nonaqueous MABs system.

| Positive electrode | Current density (mA·g1) | Discharge capacity (mAh·g1) | Cycle number |
| --- | --- | --- | --- |
| Te (This work) | 1000 | 414 | 500 |
| Te (This work) | 1000 | 492 | 300 |
| Te[1] | 500 | ~200 | 200 |
| N-PC-rGO-Te[2] | 500 | 467 | 150 |
| TeNWs/rGO[3] | 1000 | 474 | 100 |
| Te[4] | 1000 | 400 | 300 |
| NiTe[5] | 500 | 307 | 100 |
| CoTe2@N-PC[6] | 200 | 168.6 | 200 |
| ACC/S[7] | 50 | 1000 | 20 |
| CNF/S[8] | C/20 | 600 | 10 |
| S@CMK[9] | 100 | 500 | 100 |
| Se@CMK[10] | 100 | 178 | 50 |
| Se@CW[11] | 500 | 162.9 | 200 |
| Se/GA[12] | 1000 | 176 | 50 |
| TiO2@Se[13] | 500 | 225.8 | 500 |
| MCFs@Se[14] | 1000 | 230 | 100 |

References

[1]	H. D. Jiao, D. H. Tian, S. J. Li, C. P. Fu and S. Q. Jiao, A rechargeable Al–Te battery, ACS Appl. Energy Mater., 1(2018), No. 9, p. 4924.

[2]	X. F. Zhang, M. Y. Wang, J. G. Tu and S. Q. Jiao, Hierarchical N-doped porous carbon hosts for stabilizing tellurium in promoting Al–Te batteries, J. Energy Chem. 57(2021), p. 378.

[3]	X. F. Zhang, S. Q. Jiao, J. G. Tu, W.L. Song, X. Xiao, S. J. Li, M. Y. Wang, H. P. Lei, D. H. Tian, H. S. Chen and D. N. Fang, Rechargeable ultrahigh-capacity tellurium–aluminum batteries, Energy Environ. Sci.,12(2019), No. 6, p. 1918.

[4]	X. F. Zhang, J. G. Tu, M. Y. Wang and S. Q. Jiao, A strategy for massively suppressing the shuttle effect in rechargeable Al–Te batteries, Inorg. Chem. Front.,7(2020), No. 20, p. 4000.

[5]	Z. Y. Yu, S. Q. Jiao, J. G. Tu, Y. W. Luo,W. L. Song, H. D. Jiao, M. Y. Wang, H. S. Chen and D. N. Fang, Rechargeable nickel telluride/aluminum batteries with high capacity and enhanced cycling performance, ACS Nano, 14(2020), No. 3, p. 3469.

[6]	B. Zhang, Y. Zhang, J. Li, J. Liu, X. Huo and F. Kang, In situ growth of metal–organic framework-derived CoTe2 nanoparticles@ nitrogen-doped porous carbon polyhedral composites as novel cathodes for rechargeable aluminum-ion batteries, J. Mater. Chem. A, 8(2020), No. 11, p. 5535.

[7]	T. Gao, X. Li, X. Wang, J. Hu, F. Han, X. Fan, L. Suo, A. J. Pearse, S. B. Lee and G. W. Rubloff, A rechargeable Al/S battery with an ionic‐liquid electrolyte, 128(2016), Angew Chem., No. 34, p. 10052.

[8]	X. Yu and A. Manthiram, Electrochemical energy storage with a reversible nonaqueous room‐temperature aluminum–sulfur chemistry, Adv. Energy Mater., 7(2017), No. 18, p.1700561.

[9]	W. Chu, X. Zhang, J. Wang, S. Zhao, S. Liu and H. Yu, A low-cost deep eutectic solvent electrolyte for rechargeable aluminum–sulfur battery, Energy Storage Materials, 22(2019), p. 418.

[10]	X. Huang, Y. Liu, C. Liu, J. Zhang, O. Noonan and C. Yu, Rechargeable aluminum–selenium batteries with high capacity, Chem. Sci., 9(2018), No. 23, p. 5178.

[11]	Z. Li, J. Liu, X. Huo, J. Li and F. Kang, Novel one-dimensional hollow carbon nanotubes/selenium composite for high-performance Al-Se batteries, ACS Appl. Mater., 11(2019), No. 49, p. 45709.

[12]	T. Zhang, T. Cai, W. Xing,T . Li, B. Liang, H. Hu, L. Zhao, X. Li and Z. Yan, A rechargeable 6-electron Al–Se battery with high energy density, Energy Storage Mater., 41(2021), p. 667.

[13]	Z. Li, X. Wang, X. Li and W. Zhang, Reduced graphene oxide (rGO) coated porous nanosphere TiO2@Se composite as cathode material for high-performance reversible Al-Se batteries, Chem. Eng. J., 400(2020), p. 12600.

[14]	Y. Kong, A. K. Nanjundan, Y. Liu, H. Song, X. Huang and C. Yu, Modulating ion diffusivity and electrode conductivity of carbon nanotube@mesoporous carbon fibers for high performance aluminum–selenium batteries, Small, 15(2019), No. 51, p. 1904310.