Supporting Information

High-temperature corrosion of sintered RE2Si2O7 (RE = Yb and Ho) environmental barrier coating materials by volcanic ash

Ayahisa Okawa1),, Son Thanh Nguyen2), Tadachika Nakayama3),, Thi-Mai-Dung Do3), Hisayuki Suematsu3), Shu Yin1,4), Takuya Hasegawa1), Tsuneo Suzuki3), Takashi Goto3), and Koichi Niihara3)

1) Institute of Multidisciplinary Research for Advanced Materials, Tohoku University, Sendai 980-8577, Japan

2) Department of Creative Engineering, National Institute of Technology, Kushiro 084-0916, Japan

3) Extreme Energy-Density Research Institute, Nagaoka University of Technology, Nagaoka 940-2188, Japan

4) Advanced Institute for Materials Research (WPI-AIMR), Tohoku University, Sendai 980-8577, Japan

(Received: 31 October 2023; revised: 27 March 2024; 2 April 2024)

Corresponding authors: Ayahisa Okawa   E-mail: ayahisa.okawa@tohoku.ac.jp; Tadachika Nakayama    E-mail: nky15@vos.nagaokaut.ac.jp

Table S1. Full chemical compositions of as-collected volcanic ash       mol%

| SiO2 | Al2O3 | CaO | MgO | Na2O | Fe2O3 | K2O | TiO2 | MnO | SO3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 64.2 | 11.8 | 9.3 | 4.8 | 4.1 | 3.6 | 1.1 | 0.6 | 0.2 | 0.2 |

Fig. S1. (a) DTA results of volcanic ash and (b) XRD pattern of as-collected Kagoshima volcanic ash.

Fig. S2. Schematic illustration of XRD measurement.

Fig. S3. Surface images of (a–c) Yb2Si2O7 and (d–f) Ho2Si2O7 after heat treatment at 1400℃.

Fig. S4. Elemental mapping near the tip of volcanic ash penetration of the cross-section of Yb2Si2O7 after heat treatment at 1400℃ for 24 h (The top refers to the surface direction, while the bottom direction indicates the internal aspect).