Supporting Information

Polypyrrole-coated triple-layer yolk-shell Fe2O3 anode materials with their enhanced cycling stability and capacity in lithium-ion batteries

Zhen He1), Jiaming Liu1), Yuqian Wei1), Yunfei Song1), Wuxin Yang2), Aobo Yang2), Yuxin Wang1),, and Bo Li2),

1) School of Materials Science and Engineering, Jiangsu University of Science and Technology, Zhenjiang 212000, China

2) Department of Chemical &Materials Engineering, the University of Auckland, Auckland 1010, New Zealand

(Received: 22 February 2024; revised: 31 May 2024; accepted: 6 June 2024)

Corresponding authors: Yuxin Wang E-mail: ywan943@163.com;  Bo Li E-mail: bli219@aucklanduni.ac.nz

Fig. S1.  Scanning electron microscopy (SEM) image of carbon sphere acted as a template, d: diameter.

The cyclic voltammetry (CV) curve of the Fe2O3-TLY in Fig. S2 demonstrates a pronounced reduction peak at 0.75 V during the initial cathodic scan. This substantial reduction peak is attributed to the embedding of Li+ ions, forming LixFe2O3, followed by a conversion reaction where Fe3+/Fe2+ is reduced to Fe [1]. Subsequent irreversible reduction peaks at 1.03 V and 1.63 V are owing to the formation of the solid electrolyte interface (SEI) layer [2] and Li+ insertion into the Fe2O3 lattices [3]. In the anodic scan, reversible oxidation peaks at 1.68 V and 1.86 V correspond to the delithiation process where Fe is oxidized to Fe3+[4]. In subsequent cycles, the reduction and oxidation peaks stabilize around 0.80 V and 1.56 V, indicating good redox reversibility [5]. The prominent reduction peak shifts from 0.75 V to 0.80 V, and the peak height decreases due to irreversible structural rearrangement and electrolyte loss during the formation of the SEI layer in the first cycle.

Fig. S2.  CV curve of the Fe2O3-TLY electrode at a scan rate of 0.1 mV·s1.

Fig. S3.  Charge–discharge curves of the (a) Fe2O3@Ppy-TLY and (b) Fe2O3-TLY electrodes at 1 C running after different cycles.

Fig. S4.  Charge–discharge curves of the (a) Fe2O3@Ppy-TLY and (b) Fe2O3-TLY electrodes at different current densities.

Fig. S5.  Long cycling performance of Fe2O3@Ppy-TLY electrode at 6 C, after rate performance test.

Fig. S6.  Transmission electron microscopy (TEM) image of Fe2O3@Ppy-TLY electrode after 50 cycles at 0.2 C.

Table S1.  Impedance parameters recorded on Fe2O3@Ppy-TLY and Fe2O3-TLY electrodes before and after 250 cycles

| Situation | Sample | Rct / Ω | CPE1 / F | CPE1 / F |
| --- | --- | --- | --- | --- |
| After cycling | Fe2O3@Ppy-TLY | 22.01 | 3.05×105 | 0.82 |
|  | Fe2O3-TLY | 193.7 | 5.15×105 | 0.70 |
| Before cycling | Fe2O3@Ppy-TLY | 51.35 | 4.89×105 | 0.75 |
|  | Fe2O3-TLY | 74.74 | 5.16×105 | 0.71 |

CPE1 represents capacitance, and CPE2 is the degree of similarity to a pure capacitor; Rct is the charge transfer impedance.

References

[1] F.X. Ma, H.B. Wu, C.Y. Xu, L. Zhen and X.W. (David) Lou, Self-organized sheaf-like Fe3O4/C hierarchical microrods with superior lithium storage properties, Nanoscale, 7(2015), No.10, p.4411.

[2] Z.C. Yang, J.G. Shen, and L.A. Archer, An in situ method of creating metal oxide–carbon composites and their application as anode materials for lithium-ion batteries, J. Mater. Chem., 21(2011), No. 30, p. 11092.

[3] J.Y. Mao, D.C. Niu, N. Zheng, et al., Fe3O4-embedded and N-doped hierarchically porous carbon nanospheres as high-performance lithium ion battery anodes, ACS Sustainable Chem. Eng., 7(2019), No. 3, p. 3424.

[4] Y. Yang, J.Q. Li, D.Q. Chen, and J.B. Zhao, A facile electrophoretic deposition route to the Fe3O4/CNTs/rGO composite electrode as a binder-free anode for lithium ion battery, ACS Appl. Mater. Interfaces, 8(2016), No. 40, p. 26730.

[5] P. Huang, W. Tao, H.X. Wu, et al., N-doped coaxial CNTs@α-Fe2O3@C nanofibers as anode material for high performance lithium ion battery, J. Energy Chem., 27(2018), No. 5, p. 1453.