Supplementary Information

Self-supporting and hierarchically porous NixFe–S/NiFe2O4 heterostructure as a bifunctional electrocatalyst for fluctuating overall water splitting

Wenjing Yan1), Jintao Zhang1), Aijing Lv1), Songle Lu1), Yiwei Zhong1), , and Mingyong Wang1,2), 

- State Key Laboratory of Advanced Metallurgy, University of Science and Technology Beijing, Beijing 100083, China

- Beijing Key Laboratory of Green Recovery and Extraction of Rare and Precious Metals, University of Science and Technology Beijing, Beijing 100083, China

Corresponding authors: Yiwei Zhong E-mail: ywzhong@ustb.edu.cn; Mingyong Wang   E-mail: mywang@ustb.edu.cn

Possible reaction equations of chemical sulfuration：

| NiO + Na2S + H2O = NiS + 2NaOH | ∆G= -38.196 kJ | (S1) |  |
| --- | --- | --- | --- |
| FeO + Na2S + H2O = FeS + 2NaOH | ∆G= -19.516 kJ |  | (S2) |
| Fe2O3 + 3Na2S + 3H2O = Fe2S3 + 6NaOH | ∆G= -33.945 kJ |  | (S3) |
| Fe2O3 + 3Na2S + 3H2O = FeS + FeS2 + 6NaOH | ∆G= -12.506 kJ |  | (S4) |

Fig. S1 SEM images of (a, b) porous NiFe alloy, (c, d) NiFe oxides, (e) Ni1/2Fe–S/NiFe2O4 at low magnification, Insets in (b) and (d) are the magnification images. Inset in (e) is the optical photo of CC with Ni1/2Fe–S/NiFe2O4.

Fig. S2 The dependence of morphology on Ni content. (a) Fe–S/Fe2O3, (b) Ni1/5Fe–S/NiFe2O4, (c) Ni1/2Fe–S/NiFe2O4, (d) Ni4/5Fe–S/NiFe2O4, (e) Ni–S/Ni-O.

Fig. S3 Linear scanning voltammogram (LSV) by reverse scan in 1 mol L-1 KOH of NixFe–S/NiFe2O4, Ni–S/NiO, Fe–S/Fe2O3, NiFe, NiFe2O4, IrO2–Ta2O5 and Ni1/2Fe–S.

Fig. S4 OER performance of NixFe–S/NiFe2O4 with x value of 1/5 to 4/5 in 1 mol L-1 KOH. Linear scanning voltammogram (LSV) by (a) forward scan and reverse scan. (c) The corresponding Tafel plots obtained by forward scan.

Fig. S5 Cyclic voltammetry curves of (a) NiFe, (b) NiFe2O4, (c) Ni–S/NiO, (d) Fe–S/Fe2O3, (e) Ni4/5Fe–S/NiFe2O4, (f) Ni3/4Fe–S/NiFe2O4, (g) Ni1/2Fe–S/NiFe2O4, (h) Ni1/4Fe–S/NiFe2O4, (i) Ni1/5Fe–S/NiFe2O4, (f) Ni1/2Fe–S. Scanning rates: 10–80 mV·s-1.

Fig. S6 Chronopotentiometric curves of Ni1/2Fe–S/NiFe2O4 electrode for OER at 20 mA·cm-2 and 50 mA·cm-2.

Fig. S7 Cyclic voltammetry curves of unactivated Ni1/2Fe–S/NiFe2O4 at 1st, 3rd, 50th and 80th cycles.

Fig. S8 HER performance of NixFe–S/NiFe2O4 in 1 mol/L KOH. (a) linear scanning curves. (b) The corresponding Tafel plots.

Fig. S9 Nyquist plots of Ni1/5Fe–S/NiFe2O4, Ni–S/NiO, Fe–S/Fe2O3, Ni1/5Fe–S and NiFe2O4 for HER.

Fig. S10 Chronopotentiometric curves of Ni1/5Fe–S/NiFe2O4 electrode for HER at 20 mA·cm-2 and 50 mA/cm2.

Fig. S11 Photo of Ni1/5Fe–S/NiFe2O4||Ni1/2Fe–S/NiFe2O4 electrolyzer for overall water splitting.

Table S1 OER performance of NixFe–S/NiFe2O4 in 1 mol L-1 KOH solution.

| Catalysts | Forward scan |  |  | Reverse scan |  | Tafel slope (mV dec-1) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | η10(mV) | η50(mV) | η10(mV) η50(mV) |  |  |
| NiFe |  | 358 | 555 | 363 | 562 | 63 |
| NiFe2O4 |  | 321 | 583 | 335 | 584 | 75 |
| Ni–S/NiO |  | 414 | 625 | 418 | 627 | 94 |
| Fe–S/Fe2O3 |  | 425 | 640 | 429 | 640 | 102 |
| Ni1/2Fe–S |  | 303 | 492 | 312 | 495 | 79 |
| Ni1/5Fe–S/NiFe2O4 |  | 304 | 467 | 313 | 473 | 86 |
| Ni1/4Fe–S/NiFe2O4 |  | 259 | 455 | 291 | 458 | 71 |
| Ni1/2Fe–S/NiFe2O4 |  | 248 | 396 | 267 | 397 | 52 |
| Ni3/4Fe–S/NiFe2O4 |  | 275 | 445 | 302 | 306 | 86 |
| Ni4/5Fe–S/NiFe2O4 |  | 309 | 484 | 317 | 485 | 73 |
| IrO2 |  | 398 | 536 | 398 | 538 | 77 |

Table S2  Cdl results calculated from CV curves.

| sample | NiFe | Ni1/2Fe–S | Fe–S/Fe2O3 | Ni3/4Fe–S/NiFe2O4 | Ni1/4Fe–S/NiFe2O4 |
| --- | --- | --- | --- | --- | --- |
| Cdl (mF·cm-2) | 4.2 | 13.5 | 9.9 | 16.9 | 19.4 |
| sample | NiFe2O4 | Ni–S/NiO | Ni4/5Fe–S/NiFe2O4 | Ni1/2Fe–S/NiFe2O4 | Ni1/5Fe–S/NiFe2O4 |
| Cdl (mF·cm-2) | 7.6 | 9.6 | 15 | 40.8 | 16.1 |