Supplementary Information

Microscale mechanism of tailing thickening in metal mines

Huazhe Jiao1,2), Wenbo Yang1), Zhu’en Ruan2),, Jianxin Yu1), Juanhong Liu2), and Yixuan Yang1)

1) School of Civil Engineering, Henan Polytechnic University, Jiaozuo 454000, China

2) School of Civil and Resource Engineering, University of Science and Technology Beijing, Beijing 100083, China

Corresponding author: Zhu’en Ruan   E-mail: ustb_ruanzhuen@hotmail.com

Table S1.  Pilot-scale continuous thickener

| Component | Dimensions and parameters |
| --- | --- |
| Settlement column | Diameter 10 cm, height 100 cm |
| Flocculant feed pump | BS100-1A |
| Agitator | Height 60 cm, width 10 cm |
| Rake | Height 90 cm, width 8 cm |
| Low speed motor | Speed 0–10 r/min |

Fig. S1.  Continuous shear thickening test: (a) slurry preparation, (b) settling column, (c) flocculation–sedimentation, (d) deposited bed, (e) tailing bed sampling, and (f) tailing specimen.

Fig. S2.  Rotating reverse seepage test device: (a) experimental device scheme and (b) layout of the laboratory device

Fig. S3.  Reverse seepage test device.

Fig. S4.  Three-dimensional reconstruction process: (a) slice chart, (b) threshold segmentation, (c) binarization, (d) 3D reconstruction, (e) pore network model, and (f) channel characterization.

Table S2.  Details of PNM

| Parameters |  | S1 | S2 |  | S3 |  | S4 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model size / mm |  | 2×2×2 | 2×2×2 | 2×2×2 |  | 2×2×2 |  |
| Shearing time / min |  | 0 | 10 |  | 30 |  | 60 |
| Model porosity |  | 0.494 | 0.358 |  | 0.302 |  | 0.277 |
| Number of spheres |  | 1332 | 1229 |  | 1089 |  | 806 |
| Number of throats |  | 525 | 478 |  | 371 |  | 339 |
| Radius of sphere / μm | Minimum value | 0.85 | 0.78 |  | 0.53 |  | 0.26 |
|  | Maximum value | 117.62 | 115.02 |  | 106.11 |  | 94.66 |
|  | Average value | 76.79 | 73.21 |  | 68.65 |  | 66.36 |
| Radius of throat / μm | Minimum value | 0.93 | 0.91 |  | 0.56 |  | 0.25 |
|  | Maximum value | 94.69 | 87.61 |  | 86.52 |  | 83.75 |
|  | Average value | 28.66 | 31.34 |  | 25.12 |  | 20.78 |
| Coordination number of pore throat | Minimum coordination number | 2 | 1 |  | 1 |  | 1 |
|  | Maximum coordination number | 35 | 35 |  | 32 |  | 25 |
|  | Average coordination number | 10.83 | 11.07 |  | 9.16 |  | 7.39 |
| Radius ratio of pore throat | Minimum value | 1 | 1 |  | 1 |  | 1 |
|  | Maximum value | 23.18 | 2.95 |  | 3.71 |  | 3.78 |
|  | Average value | 2.69 | 2.34 |  | 2.74 |  | 3.19 |

Fig. S5.  Observation of the tailings bed shear thickening process.

Fig. S6.  Evolution of the seepage flow channel.

Table S3.  Boundary parameters

| Fluid density, / (kg∙m3) | Dynamic viscosity, μ / (Pa∙s) | Inlet pressure, Pin / Pa | Outlet pressure, Pout / Pa | Model size, V / mm3 |
| --- | --- | --- | --- | --- |
| 1000 | 0.001 | 1.3 × 105 | 1.0 × 105 | 1 |

Table S4.  Reserve direction seepage simulation result

| Specimen |  | S1 | S2 | S3 | S4 |
| --- | --- | --- | --- | --- | --- |
| Sampling time / min |  | 0 | 10 | 30 | 60 |
| Number of flow lines |  | 452 | 489 | 423 | 363 |
| Absolute permeability / (10−3 μm2) |  | 13.70 | 14.32 | 11.07 | 10.63 |
| Pressure value / Pa | Maximum value | 129724 | 129866 | 129852 | 129906 |
|  | Minimum value | 98820 | 99445 | 101107 | 101933 |
|  | Average value | 104565 | 108246 | 114916 | 116794 |
| Velocity value / (μm∙s) | Maximum value | 1.457 | 1.537 | 1.183 | 1.038 |
|  | Minimum value | 1.162 | 1.182 | 1.025 | 1.002 |
|  | Average value | 1.283 | 1.302 | 1.104 | 1.020 |