Supplementary Information

Effects of iron oxide on crystallization behavior and spatial distribution of spinel in stainless steel slag

Zihang Yan1,2), Qing Zhao1,2),, Chengzhi Han1,2), Xiaohui Mei1,2), Chengjun Liu1,2), and Maofa Jiang1,2)

1) Key Laboratory for Ecological Metallurgy of Multimetallic Mineral (Ministry of Education), Northeastern University, Shenyang 110819, China

2) School of Metallurgy, Northeastern University, Shenyang 110819, China

 Corresponding author: Qing Zhao     E-mail: zhaoq@smm.neu.edu.cn

Fig. S1.  Experimental apparatus used in the study. (a) High temperature quenching furnace. 1–fixed valve; 2–gas outlet; 3–airtight valve; 4–furnace cover; 5–molybdenum wire; 6–corundum tube; 7–MgO crucible; 8–thermocouple A; 9–water outlet; 10–gas inlet; 11–sealing cover A; 12–thermocouple B; 13–sealing cover B; 14–water inlet; 15–insulation layer; 16–heating elements; 17–sample; 18–sealing clip. (b) High temperature tube furnace. 1–sample; 2–charging cylinder; 3–corundum tube; 4–furnace cover; 5–insulation layer; 6–graphite crucible; 7–thermocouple A; 8–water outlet; 9–furnace base; 10–gas inlet; 11–heating elements; 12–MgO crucible; 13–sample; 14–refractory; 15–water inlet; 16–thermocouple B;

Fig. S2.  XRD patterns of water quenched slag samples (1600°C) with 8wt% and 18wt% FeO contents.