Supplementary Information

# Insight to the enhanced microwave absorption of porous N-doped carbon driven by ZIF-8: Competition between graphitization and porosity

You Zhou, Hongpeng Wang, Dan Wang, Xianfeng Yang, Hongna Xing, Juan Feng, Yan Zong, Xiuhong Zhu, Xinghua Li(, and Xinliang Zheng

School of Physics, State Key Laboratory of Photoelectric Technology and Functional Materials, Northwest University, Xi’an 710127, China

(Corresponding author: Xinghua Li   E-mail: xinghua.li@nwu.edu.cn

Fig S1. XRD patterns of NPC materials after deducting the background.

Table S1.  XRD parameters of NPC materials

| Sample | FWHM | Position of peaks | Intensity of peaks (a.u.) |
| --- | --- | --- | --- |
|  | (002) | (100) | (002) | (100) | (002) | (100) |
| NPC-800 | 5.55 | 9.27 | 24.82° | 44.75° | 877 | 233 |
| NPC-900 | 5.45 | 9.14 | 24.55° | 44.31° | 1218 | 319 |
| NPC-1000 | 5.07 | 8.96 | 23.56° | 44.10° | 1302 | 388 |
| NPC-1100 | 4.46 | 8.73 | 23.35° | 43.92° | 1505 | 538 |
| NPC-1200 | 4.24 | 8.01 | 22.89° | 43.83° | 1789 | 679 |

Fig S2. Cole-Cole curves of NPC materials.

Table S2. Comparison of microwave absorption performance between NPC in this work and other Zn-based MOFs derived NPC composites

| Sample | wt (%) | Thickness (mm) | f (GHz) | RLmin (dB) | EAB （GHz） | References |
| --- | --- | --- | --- | --- | --- | --- |
| PPy/ZIFs | 30 | 2.9 | ~12 | -49 | 6.2 | [1] |
| porous ZnO/C nanofiber | 20 | 1.5 | 16.2 | -22.89 | 5.64 | [2] |
| CoFe alloys@ZnO@C | 30 | 2.2 | -- | -40.63 | -- | [3] |
| ZIF-8@ZIF-67 | 50 | 1.9 | ~16 | -28.8 | 4.2 | [4] |
| ZnO-Ni@C | 50 | 2.3 | 10.6 | -58.6 | 4.8 | [5] |
| N-doped porous carbon | 50 | 4 | 8.5 | -39.7 | 4.3 | [6] |
| CNT/RGO/ZIF-8 | 25 | 4.5 | 6.5 | -39.2 | -- | [7] |
| ZnO/NPC/RGO | 40 | 2.4 | 14 | -50.5 | ~6 | [8] |
| CoO/Co/C (Co/Zn-ZIFs) | 25 | 3.3 | 7.2 | -66.7 | -- | [9] |
| NPC-800 | 25 | 1.29 | 17.0 | -50.57 | 4.17 | This work |

References

[1]	Y. Z. Jiao, J. J. Li, A. M. Xie, F. Wu, K. Zhang, W. Dong, and X. F. Zhu. Confined polymerization strategy to construct polypyrrole/zeolitic imidazolate frameworks (PPy/ZIFs) nanocomposites for tunable electrical conductivity and excellent electromagnetic absorption. Compos. Sci. Technol., 174(2019), p 232-240.

[2]	W. H. Gu, J. Lv, B. Quan, X. H. Liang, B. S. Zhang, and G. B. Ji. Achieving MOF-derived one-dimensional porous ZnO/C nanofiber with lightweight and enhanced microwave response by an electrospinning method. J. Alloy Compd., 806(2019), p 983-991.

[3]	M. Y. Kong, X. H. Liu, Z. R. Jia, B. B. Wang, X. M. Wu, and G. L. Wu. Porous magnetic carbon CoFe alloys@ZnO@C composites based on Zn/Co-based bimetallic MOF with efficient electromagnetic wave absorption. J. Colloid Interface Sci., 604(2021), p 39-51.

[4]	X. H. Liang, B. Quan, G. B. Ji, W. Liu, Y. Cheng, B. S. Zhang, and Y. W. Du. Novel nanoporous carbon derived from metal-organic frameworks with tunable electromagnetic wave absorption capabilities. Inorg. Chem. Front., 3(2016), p 1516-1526.

[5]	Y. C. Zhang, S. T. Gao, H. L. Xing, and H. X. Li. In situ carbon nanotubes encapsulated metal nickel as high-performance microwave absorber from Ni-Zn metal-organic framework derivative. J. Alloy Compd., 801(2019), p 609-618.

[6]	Q. L. Wu, H. H. Jin, W. Chen, S. Q. Huo, X. Chen, X. G. Su, H. Wang, and J. Wang. Graphitized nitrogen-doped porous carbon composites derived from ZIF-8 as efficient microwave absorption materials. Mater. Res. Express, 5(2018), p 065602.

[7]	J. X. Wang, J. F. Yang, J. Yang, and H. Zhang. Design of novel CNT/RGO/ZIF-8 ternary hybrid structure for lightweight and highly effective microwave absorption. Nanotechnology, 31(2020), p 414001.

[8]	X. H. Liang, B. Quan, G. B. Ji, W. Liu, H. Q. Zhao, S. S. Dai, J. Lv, and Y. W. Du. Tunable dielectric performance derived from the metal-organic framework/reduced graphene oxide hybrid with broadband absorption. ACS Sustain. Chem. Eng., 5(2017), p 10570-10579.

[9]	R. W. Shu, W. J. Li, Y. Wu, J. B. Zhang, G. Y. Zhang, and M. D. Zheng. Fabrication of nitrogen-doped cobalt oxide/cobalt/carbon nanocomposites derived from heterobimetallic zeolitic imidazolate frameworks with superior microwave absorption properties. Compos. B. Eng., 178(2019), p 107518.