Supplementary Information

Chitosan derived carbon membranes as protective layers on zinc anodes for aqueous zinc batteries

Haichao Li, Zengwu Wei, Yu Xia, Junshan Han(, and Xing Li(

School of Materials Science and Chemical Engineering, Ningbo University, Ningbo 315211, China

( Corresponding authors: Junshan Han    E-mail: jshan10@163.com;    Xing Li    E-mail: lixing@nbu.edu.cn

Fig. S1. BET images of CS-800 after high temperature sintering.

Fig. S2. XRD patterns of Zn anode after cycling, Zn, and (Zn(OH)2)3(ZnSO4)(H2O)5.

Table. S1. Comparison of four zinc batteries’ cycling times, current densities, energy densities, and polarization voltages

| Sample | Cycling time / h | Current density / (mA·cm−2) | Energy density / (mAh·cm−2) | Polarization voltage / mV |
| --- | --- | --- | --- | --- |
| ZBs-CS800 | 700 | 0.25 | 0.25 | 29 |
| Zn/rGO [1] | 300 | 0.2 | 0.3 | - |
| 100TiO2@Zn [2] | 150 | 1 | 1 | 57.2 |
| Zn/Se2O3 [3] | 270 | 0.5 | 0.5 | 48 |

References

[1] T.T. Wang, C.P. Li, X.S. Xie, B.G. Lu, Z.X. He, S.Q. Liang, and J. Zhou, Anode materials for aqueous Zinc ion batteries: mechanisms, properties, and perspectives, ACS. Nano, 14(2020), No. 12, p. 16321.

[2] K.N. Zhao, C.X. Wang, Y.H. Yu, M.Y. Yan, Q.L. Wei, P. He, Y.F. Dong, Z.Y. Zhang, X.D. Wang, and L.Q. Mai, Ultrathin Surface Coating Enables Stabilized Zinc Metal Anode, Adv. Mater. Interfaces, 5(2018), No. 16, art. No. 1800848.

[3] M. Zhou, S. Guo, G.Z. Fang, H.M. Sun, X.X. Cao, J. Zhou, A.Q. Pan, and S.Q. Liang, Suppressing by-product via stratified adsorption effect to assist highly reversible zinc anode in aqueous electrolyte, J. Energy Chem., 55(2021), p. 549.