Supplementary Information

Solid Bi2O3-derived nanostructured metallic bismuth with high formate selectivity for the electrocatalytic reduction of CO2

Xiaoyan Wang1), Safeer Jan1), Zhiyong Wang1), and Xianbo Jin1,2)

1) College of Chemistry and Molecular Sciences, Hubei Key Laboratory of Electrochemical Power Sources, Wuhan University, Wuhan 430061, China

2) Engineering Research Center of Organosilicon Compounds & Materials, Ministry of Education, Wuhan 430061, China

(a)

mBO

2 μm

nBO

(b)

500 nm

(c)

1 μm

1 μm

(d)

Fig. S1. SEM images: (a) mBO; (b) nBO; (c) mBO membrane electrode; (d) nBO membrane electrod.

Total current densitytotal / mA cm-2

0

10

20

30

40

50

60

-0.6

-0.7

-0.8

-0.9

-1.0

-1.1

-1.2

mBO-nBo

nBO-nBo

Potential / V vs. RHE

Fig. S2. Total current density for the electrochemical CO2 reduction performance of different nBi catalysts.

Fig. S3. I-t curves for the electrochemical CO2 reduction performance of (a) nBO-nBi and (b) mBO-nBi catalysts.

Fig. S4. I–t curves (a) and the FEs of electrolytic products (b) for the electrochemical CO2 reduction performance of nBO.

1 μm

(b)

(c)

200 nm

(d)

200 nm

(e)

1 μm

(f)

200 nm

1 μm

(g)

80

70

60

50

40

10

30

20

2 θ / (°)

Intensity / a.u.

(a)

-Bi2O2CO3 -Bi -Ti

(h)

200 nm

-0.88 V

-0.78 V

-0.68 V

Fig. S5. (a) XRD patterns of nBO after the 2 hours electrolysis of CO2 at differernt potentials. (b-d) SEM images of nBO after electrolysis of CO2 at -0.68 V. (e-f) SEM images of nBO after electrolysis of CO2 at -0.78 V. (g-h) SEM images of nBO after electrolysis of CO2 at -0.88 V.

Table S1 Catalytic performance of various catalysts for CO2 reduction to formate.

| Catalysts | Electrolyte | Potential (V vs. RHE) | jformate (mAcm-2) | FEformate (%) | Reference |
| --- | --- | --- | --- | --- | --- |
| Bi-Doped SnO nanosheets | 0.1 M KHCO3 | -1.7 V vs. Ag/AgCl | About 11 | 93% | [1] |
| Sn0.80Bi0.20@Bi-SnOx | 0.5 M KHCO3 | -0.88 | 20.9 | 95.8 | [2] |
| Nano architectured dendritic Bi | 0.5 M KHCO3 | -0.82 | 18.8 | 98% | [3] |
| Bi NP@ MWCNT | 0.5 M KHCO3 | -1.5 V vs. SCE | 10.2 | 95.2% | [4] |
| Cu@Bi nanocone | 0.5 M KHCO3 | -0.95 V | 30.9 | 96.9% | [5] |
| Bi nanoparticles Embedded in N-doped porous carbon | 0.1 M KHCO3 | -1.5 V vs. SCE | 14.4 | 92% | [6] |
| Bi-MWCNT-COOH composite | 0.5 M KHCO3 | -0.76 | About 6.8 | 91.7% | [7] |
| Cu nanowire bridged Bi nanosheet | 0.5 M KHCO3 | -0.86 | About 6.2 | 87% | [8] |
| AgBi-500 | 0.1 M KHCO3 | -0.7 | 12.5 | 94.3% | [9] |
| Bi nanoparticles/graphene | 0.5 M KHCO3 | -0.97 | 22.5 | 92.1% | [10] |
| Wavy SnO2 | 0.5 M KHCO3 | -1.0 | 22 | 87.4% | [11] |
| Ultrathin SnS nanosheets | 0.5 M KHCO3 | -1.1 | 18.9 | 82.1% | [12] |
| Bismuth derivatives from Bi2S3 | 0.5 M KHCO3 | -1.0 | About 7 | 80% | [13] |
| mBO-nBi | 0.5 M KHCO3 | -0.78 -0.98 | 7.3 34.3 | 97.6% 93% | This work |
| nBO-nBi | 0.5 M KHCO3 | -0.73 -0.88 | 7.5 23.1 | 97.2% 91% | This work |

References

[1]  X.W. An, S.S. Li, A. Yoshida, T. Yu, Z.D. Wang, X.G. Hao, A. Abudula, and G.Q. Guan, Bi-doped SnO nanosheets supported on Cu foam for electrochemical reduction of CO2 to HCOOH. ACS Appl. Mater. Interfaces, 11(2019), No. 45, p. 42114.

[2]  Q. Yang, Q.L. Wu, Y. Liu, S.P. Luo, X.T. Wu, X.X. Zhao, H.Y. Zou, B.H. Long, W. Chen, Y.J. Liao, L.X. Li, P.K. Shen, L. Duan, and Z.W. Quan, Novel Bi-doped amorphous SnOx nanoshells for efficient electrochemical CO2 reduction into formate at low overpotentials, Adv. Mater., 32(2020), No. 36, p. 2002822.

[3]  M.Y. Fan, S. Prabhudev, S. Garbarino, J.L. Qiao, G.A. Botton, D.A. Harrington, A.C. Tavares, and D. Guay, Uncovering the nature of electroactive sites in nano architectured dendritic Bi for highly efficient CO2 electroreduction to formate, Appl. Catal. B, 274(2020), p. 119031.

[4]  X. Zhang, J. Fu, Y.Y. Liu, X.D. Zhou, and J.L. Qiao, Bismuth anchored on MWCNTs with controlled ultrafine nanosize enables high-efficient electrochemical reduction of carbon dioxide to formate fuel, ACS Sustain. Chem. Eng., 8 (2020), No.12, p. 4871.

[5]  F.H. Zhang, C.Z. Chen, S.L. Yan, J.H. Zhong, B. Zhang, and Z.M. Cheng, Cu@Bi nanocone induced efficient reduction of CO2 to formate with high current density, Appl. Catal. A: Gen., 598(2020), p. 117545.

[6]  D.B. Zhang, Z.T. Tao, F.L. Feng, B.B. He, W. Zhou, J. Sun, J.M. Xu, Q. Wang, and L. Zhao, High efficiency and selectivity from synergy: Bi nanoparticles embedded in nitrogen doped porous carbon for electrochemical reduction of CO2 to formate, Electrochim. Acta, 334(2020), p. 135563.

[7]  Q.Q. Li, X.R. Zhang, X.D. Zhou, Q.Y. Li, H.Q. Wang, J. Yi, Y.Y. Liu, and J.J. Zhang, Simply and effectively electrodepositing Bi-MWCNT-COOH composite on Cu electrode for efficient electrocatalytic CO2 reduction to produce HCOOH, J. CO2 Util., 37(2020), p. 106.

[8]  L. Li, F.F. Cai, F.X.Y. Qi, and D.K. Ma, Cu nanowire bridged Bi nanosheet arrays for efficient electrochemical CO2 reduction toward formate, J. Alloys Compd., 841(2020), p. 155789

[9]  J.H. Zhou, K. Yuan, L. Zhou, Y. Guo, M.Y. Luo, X.Y. Guo, Q.Y. Meng, and Y.W. Zhang, Boosting electrochemical reduction of CO2 at a low overpotential by amorphous Ag-Bi-S-O decorated Bi(0) nanocrystals, Angew. Chem. Int. Ed., 58(2019), No. 40, p.14197.

[10] D. Wu, W.Y. Chen, X.W. Wang, X.Z. Fu, and J.L. Luo, Metal-support interaction enhanced electrochemical reduction of CO2 to formate between graphene and Bi nanoparticles, J. CO2 Util., 37(2020), p. 353.

[11]  Z. Chen, T.T. Fan, Y.Q. Zhang, J. Xiao, M.R. Gao, N.Q. Duan, J.W. Zhang, J.H. Li, Q.X. Liu, X.D. Yi, and J.L. Luo, Wavy SnO2 catalyzed simultaneous reinforcement of carbon dioxide adsorption and activation towards electrochemical conversion of CO2 to HCOOH, Appl. Catal. B, 261(2020), 118243.

[12]  H.L. Chen, J.X. Chen, J.C. Si, Y. Hou, Q. Zheng, B. Yang, Z.J. Li, L.G. Gao, L.C. Lei, Z.H. Wen, and X.L. Feng, Ultrathin tin monosulfide nanosheets with the exposed (001) plane for efficient electrocatalytic conversion of CO2 into formate, Chem. Sci., 11(2020), No. 15, p. 3952.

[13]  Y.T. Wang, L. Cheng, J.Z. Liu, C.Q. Xiao, B. Zhang, Q.G. Xiong, T. Zhang, Z.L. Jiang, H. Jiang, Y.H. Zhu, Y.H. Li, and C.Z. Li, Rich bismuth‐oxygen bonds in bismuth derivatives from Bi2S3 pre‐catalysts promote the electrochemical reduction of CO2, ChemElectroChem, 7(2020), No. 13, p. 2864.