Supplementary Information

Fabrication of Gd2O3-doped CeO2 thin films through DC reactive sputtering and their application in solid oxide fuel cells

Fuyuan Liang*, Jiaran Yang*, Haiqing Wang, and Junwei Wu

School of Materials Science and Engineering, Harbin Institute of Technology (Shenzhen), Shenzhen, 518055, China

*These authors contributed equally to this work.

Corresponding author: Junwei Wu          E-mail: junwei.wu@hit.edu.cn

Fig. S1. Surface (a, b) and cross-sectional (c) morphology of NiO–YSZ/YSZ half cells.

Fig. S2. Cross-sectional morphology of the annealed GDC films: (a) BSD mode; (b) SE2 mode.

Table S1. Ohmic resistance Rs and polarization resistance Rp of GDC-MS and GDC-SP tested at 800, 750, and 700℃

| Cell | 800℃ |  | 750℃ |  | 700℃ |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Rs / (Ω·cm2) | Rp / (Ω·cm2) | Rs / (Ω·cm2) | Rp / (Ω·cm2) | Rs / (Ω·cm2) | Rp / (Ω·cm2) |
| GDC-MS | 0.170 | 0.313 | 0.214 | 0.423 | 0.295 | 0.655 |
| GDC-SP | 0.278 | 0.521 | 0.381 | 0.699 | 0.569 | 1.091 |

Fig. S3. Surface morphology of screen-printed GDC buffer layer (a) and cross-sectional morphology after sintering of LSCF cathode (b).

Fig. S4. Cross-sectional SEM-EDX of (a) SUS441/MCO and (b) SUS441/GDC/MCO.

Fig. S5. ASR of SUS441/MCO annealed in air as a function of time.