Supplementary information

Sandwich-like structure C/SiOx@graphene anode material with high electrochemical performance for lithium ion batteries

Zhaolin Li1),*, Yaozong Yang1),*, Jie Wang1), Zhao Yang1), and Hailei Zhao1,2),

- School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing 100083, China

- Beijing Municipal Key Laboratory of New Energy Materials and Technologies, Beijing 100083, China

*These authors contributed equally to this work.

Fig. S1. FTIR spectra of rGO and GO.

Fig. S2. XRD pattern of SiOx@rGO material.

The lithium diffusion coefficient (DLi+) of C/SiOx@rGO electrode can be calculated based on the CV data at different scan rates (Fig. S3(c)) and the following equation (Eq. (S1)):

ip = 2.69×105·A·n3/2·C0·D1/2·ν1/2                          (S1)

where ip is the peak current (A), n is the charge concentration in LixSi (as anodic peak Ⅱ is chosen in calculation, n = 2), A is the contact area between SiOx and electrolyte (here the geometric area of electrode, 1.13 cm2, is used for simplicity), C0 is the bulk concentration of lithium in electrode (0.0549 mol/cm3, calculated from Li2Si), and ν is the scan rate. A linear relationship between ip and ν1/2 is obtained, and the diffusion coefficient of lithium ions in C/SiOx@rGO is calculated according to the slope (Fig. S3(d)). The DLi+ of C/SiOx@rGO electrode is calculated to be 1.4 × 10−12 cm2/s.

Fig. S3. Differentiate curves at different current densities of SiOx@rGO (a) and C/SiOx@rGO (b) electrodes. Cyclic voltammetry curves with different scan rates: 0.05, 0.1, 0.2, 0.3, and 0.4 mV/s (c); The relationship of the peak current (ip) and the square root of scan rate (ν1/2) (d).

Table S1. Comparison of electrochemical performance of recently reported SiOx/graphene anode materials

| Sample | Voltage range / V | ICE / % | Specific capacity / (mAh·g−1) | Current density / (A·g−1) | Cycles | Retention / % | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C/SiOx@rGO | 0.01–1.5 | 47.0 | 886 | 0.1 | 100 | 73.7 | This work |
|  |  | — | 396 | 5.0 | — | 44.7 |  |
| SiOx/rGO composite | 0.01–1.5 | 13.8 | 103 | 0.1 | 120 | 60 | [1] |
| SiOx/graphene | 0.01–3.0 | 51.7 | 1207 | 0.2 | 200 | 82.3 | [2] |
|  |  | — | 418 | 2.0 | — | 34.6 |  |
| Gr-coated SiOx | 0.01–1.5 | 71.2 | 1317 | 0.2 | 100 | 59.2 | [3] |
| Meso-porous SiOx/rGO composite | 0.01–1.5 | 68.1 | 2563 | 0.2 | 200 | 22.6 | [4] |
| Si@SiOx/graphene | 0.01–2.0 | 53.0 | 3000 | 0.1 | — | — | [5] |
|  |  | — | 1020 | 4.0 | — | 34.0 |  |
| Si@SiOx@C | 0.01–3.0 | 50.7 | 537 | 0.1 | 200 | >100 (capacity climb) | [6] |
|  |  | — | 56 | 5.0 | — | 10.4 |  |

References

- Mater. Lett., 299(2021), p. 130043.

- Electrochim. Acta, 422(2022), p. 140572.

- Chem. Eng. J., 442 (2022), p. 136166.

- Electrochim. Acta, 273(2018), p. 26.

- J. Power Sources, 306(2016), p. 42.

- Electrochim. Acta, 402(2022), p. 139556.