Supplementary Information

Improving the electrocatalytic activity of Fe, N co-doped biochar for polysulfide by regulation of N–C and Fe–N–C electronic configurations

Jingchun Sun1), Jindiao Guan1), Suqing Zhou1), Jiewei Ouyang1), Nan Zhou1,2), Chunxia Ding1), and Mei’e Zhong1),

1) School of Chemistry and Materials Science, Hunan Agricultural University, Changsha 410128, China

2) Hunan Engineering Research Center for Biochar, Hunan Agricultural University, Changsha 410128, China

Corresponding author: Mei’e Zhong        E-mail: zhongmeie@hunau.net

200 nm

200 nm

(a)

(b)

Fig. S1. SEM images of (a) OPC and (b) NOPC.

10 nm

Fig. S2. TEM image of Fe–NOPC.

100 nm

Fig. S3 SEM images of Fe–NOPC@S.

Fig. S4. Nitrogen sorption isotherms and pore size distribution (inset) of Fe–NOPC@S.

Fig. S5. (a) Galvanostatic charge–discharge profiles of the Fe–NOPC@S at various rates. (b) Cyclic stability of Fe–NOPC@S electrode. (c) Charge/discharge voltage profiles of the Fe–NOPC@S electrode at 1C.

Fig. S6. Powered by three Fe–NOPC@S batteries, 40 white LED lamps mould emit luminous optical pictures.

Fig. S7. Potentiostatic discharge curves of Li2S deposition at 2.05 V of (a) OPC and (b) NOPC.

Table S1. Elemental content from XPS analysis                                 at%

| Sample | C | N | O | P | Fe |
| --- | --- | --- | --- | --- | --- |
| OPC | 61.62 | 1.76 | 27.95 | 8.67 | — |
| NOPC | 73.08 | 3.26 | 18.01 | 5.66 | — |
| Fe–NOPC | 74.94 | 3.19 | 16.46 | 5.13 | 0.27 |

Table S2. Analysis results of XPS spectra                                wt%

| Assignment |  | OPC | NOPC | Fe–NOPC |
| --- | --- | --- | --- | --- |
| C 1s | Graphitic carbon | 72.08 | 66.74 | 66.85 |
|  | C–O/C–N | 13.28 | 15.60 | 18.46 |
|  | C=O | 14.64 | 17.66 | 14.69 |
| N 1s | Oxidized N | 45.33 | 11.13 | 15.97 |
|  | Graphitic N | 38.40 | 46.58 | 55.84 |
|  | Pyrrolic N | 12.09 | 29.91 | 13.12 |
|  | Pyridinic N | 4.18 | 12.38 | 10.02 |
|  | Fe–Nx | — | — | 5.05 |
| O 1s | Carbonyl | 11.10 | 28.12 | 34.31 |
|  | Hydroxyl | 49.06 | 57.97 | 48.10 |
|  | Carboxyl | 39.84 | 13.91 | 17.59 |
| P 2p | P–C | 36.02 | 54.61 | 28.79 |
|  | P=O | 57.92 | 39.24 | 64.25 |
|  | P–O | 6.06 | 6.15 | 6.96 |