Effect of variations in the polar and azimuthal angles of coarse particles on the structure of drainage channels in thickened beds

Cuiping Li1), Gezhong Chen1), Zhu’en Ruan1,2), (, Raimund Bürger3), Yuan Gao4), Hezi Hou1,5), and Hui Wang1,5)

- Key Laboratory of the Ministry of Education of China for High-efficient Mining and Safety of Metal Mines, University of Science and Technology Beijing, Beijing 100083, China

- Shunde Innovation School, University of Science and Technology Beijing, Foshan 528399, China

- CI2MA and Departamento de Ingeniería Matemática, Facultad de Ciencias Físicas y Matemáticas, Universidad de Concepción, Casilla 160-C, Concepción, Chile

- School of Metallurgical and Ecological Engineering, University of Science and Technology Beijing, Beijing 100083, China

- School of Civil and Resource Engineering, University of Science and Technology Beijing, Beijing 100083, China

(Corresponding author: Zhu’en Ruan   E-mail: ustb_ruanzhuen@hotmail.com

Fig. S1. Rake structure diagram (The scale is 1:1, the unit is mm.)

Fig. S2. Drainage channel threshold segmentation and calculation

Fig. S3. Pore and throat channel structure diagram: (a) Removing redundancy; (b) Throat channel structure.

Fig. S4. Coarse particle threshold segmentation and calculation

Fig. S5. Coarse particle threshold segmentation: (a) i = 60; (b) i = 50; (c) i = 39.

Fig. S6. Pore equivalent diameter variation with bed height: (a) 0 r·min-1-1 h; (b) 0 r·min-1-2 h; (c) 1 r·min-1-1 h.

Fig. S7. Throat channel equivalent radius variation with bed height: (a) 0 r·min-1-1 h; (b) 0 r·min-1-2 h; (c) 1 r·min-1-1 h.

Fig. S8. Distribution of the particle’s φ: (a) Polar angle range; (b) Particle’s φld; (c) Particle’s φbd.

Fig. S9. Variation of the particle’s φ with particle size: (a) Variation of the particle’s φld with particle size; (b) Variation of the particle’s φbd with particle size.

Fig. S10. Distribution of the particle’s θ: (a) Azimuthal angle range; (b) Particle’s θld;                   (c) Particle’s θbd.

Fig. S11. Variation of the particle’s θ with particle size: (a) Variation of the particle’s θld with particle size; (b) Variation of the particle’s θbd with particle size.

Fig. S12. The variation of bed concentration and volume ratio with bed height: (a) Concentration distribution; (b) Ratio of throat volume to pore volume; (c) Volume variation ratio.

# Text boxes

(a)

(b)

(a)

(b)

(c)

(b)

(a)

(c)

(b)

(a)

(c)

(b)

(a)

(c)

(a)

(b)

(c)

(b)

(a)

(a)

(b)

(b)

(a)

(c)